Method:

3-Point Bending Test -metal

1. Measure the width, height, and support span of 4 sheets of cast iron and 4 sheets of low carbon steel.

2. Place sample on three-point bending test device.

3. Load at specified rate and record load-displacement data until test is terminated.

4. Use the data to plot load-displacement diagrams and to calculate Young’s modulus and stiffness

Result:

We measured the average width and thickness of four samples of each metal and calculated the moments of inertia of the cross sections using the equation I=bh3/12. In addition, we recorded the crosshead velocity of the specimens and the span of the two lower supporting posts L. (Table.6)

Table 6: Procedure 3 - Dimensions of medal samples

| sample | Crosshead speed | span L | b_average (mm) | h_average (mm) | I (mm4） |
| --- | --- | --- | --- | --- | --- |
| Steel1 | 5mm/min | 60mm | 19.860. | 3.7666. | 88.444. |
| Steel2 |  |  | 19.900. | 3.6866. | 83.094. |
| Steel3 |  |  | 19.860. | 3.6733. | 82.031. |
| Steel4 |  |  | 19.833. | 3.6800. | 82.367. |
| Iron1 |  |  | 19.953. | 3.7533. | 87.919. |
| Iron2 |  |  | 20.093. | 3.7666. | 89.483. |
| Iron3 |  |  | 20.126. | 3.7400. | 87.741. |
| Iron4 |  |  | 20.100. | 3.7466. | 88.094. |

In the test, the low carbon steel bent significantly in the center and became “U” shaped, while the cast iron broke quickly with insignificant deformation. Obtaining the data of load force P and displacement δ, we can plot the load-deflection curves for the three-point bending tests (Figure 5). Fitting the straight-line portion gives the stiffness S. We have also labeled the maximum load Pmax, although no load drop has yet occurred on the low carbon steel. The curves show that cast iron broke immediately after the maximum load was reached, while low carbon steel had better toughness.

Getting the stiffness and the fracture load, we calculate Young’s Modulus by E=PL348δI=SL348I. We can also fetch the maximum moment Mmax by Mmax=PmaxL4

at the mid-span of the specimen during the whole process. Then from the beam theory σmax=Mmaxh2I, we calculate the maximum bending stress. The results are shown in Table 7. We have noted that the result[s] for the Young’s Modulus of both low carbon steel and cast iron are much smaller than what are shown in Procedure 1.

| Sample | Pmax (N) | Stiffness (N/mm) | Young’s Modulus (GPa) |
| --- | --- | --- | --- |
| Iron 1 | 1108.48 | 1071.38 | 26.78 |
| Iron 2 | 1024.03 | 959.73 | 23.99 |
| Iron 3 | 1000.63 | 971.43 | 24.29 |
| Iron 4 | 1000.04 | 1009.95 | 25.25 |
| Iron (Average) | 1033.30 | 1003.12 | 25.08 |
| Steel 1 | 2813.09 | 2279.78 | 56.99 |
| Steel 2 | 2826.47 | 2211.56 | 55.29 |
| Steel 3 | 2822.14 | 2313.14 | 57.83 |
| Steel 4 | 2827.95 | 2328.58 | 58.21 |
| Steel (Average) | 2822.41 | 2283.27 | 57.08 |

According to the t-test results, we can confirm that the Young's moduli of the two metal materials measured by the three-point bending method exhibit significant differences from those obtained via the tensile method. As shown in the following figure, the p-values of both materials are less than 0.01, which confirms the validity of our observation: the Young's modulus measured by the three-point bending method is lower than that measured by the tensile method.